Percenta Anti-Condensation for Synthetic Material

Areas of application:

Wind deflector plates of motorbikes, shower partitions, synthethic windows, visors

Percenta Anti-Condensation for Synthetic Materials is a coating material for synthetic surfaces with anti-condensation- and antistatic effect.

Dilution:	None

Quantity to be applied:	approx. 10-15 ml per m²

Curing/Drying:	approx. 1-2 minutes at least

Processing temperature:	+5°C to +25°C - to be protected against direct insolation -

Handling:	refer to safety data sheet

Storing and durability:	refer to safety data sheet, imprint on bottles or cans

Storing temperature: 	+5°C  to +25°C, to be protected against direct insolation and frost, to be stored well closed in the original container

Application:

The carrying of gloves is recommended. Percenta Anti-Condensation for Synthetics dehumidifies the skin. The application should be checked at an inconspicuous spot or a sample. Not to be applied at temperatures below +5°C.

Preparation:

The surface has to be cleaned carefully from dusty, greasy and fatty pollutions. It is recommended to use Percenta Synthetic-Cleaner or Glass SR-Cleaner. Then it should be rinsed intensively with clear water. Before coating the surfaces must be clean, dry and non-greasy.

Coating:

Put a small portion of Percenta Anti-Condensation for Synthetic Material on a dry, fluff-free towel and apply it regularly to the surface, so that a closed, thin fluid coat arises, which will dry up slowly.

Drying:

Within a short time period (approx. 1 min) the coating is dry. If after drying reams become visible, too much of the product was used. A repetition of the coating with less coating material takes out the reams and ensures high visibility

Influence of the environment:

Do only coat small surfaces at temperatures above 25°C.

Cleaning of the coated surface:

The surfaces coated with Percenta Anti-Condensation for Synthetic Material can be cleaned with mild cleaners (for example Percenta Glass SR). It is recommended to carry out a re-coating, as described above.