Percent Plastic-Sealing

Percenta Plastic-Sealing, which shows an Easy-to-Clean effect on synthetic surfaces (polyester, PMMA, PC), is a temporary alcohol-based coating material on basis of the chemical nano technology. The rubbed material causes a thin coat on the surfaces, which reduces the adherence of dirt and foreign substances, as well as le better dripping off of water. Coated surfaces can be cleaned easier.

Dilution:	none

Quantity to be applied:	approx. 10-25 ml per m²

Curing / Drying:	approx. 30 minutes at minimum, preferably 24 hours

Handling:	refer to safety data sheet

Storing and durability:	refer to safety data sheet, imprint on bottles or cans

(storing temperature: +5°C  to +25°C, to be protected against direct insolation and frost, to be stored well closed in the original container)

Application:

The carrying of gloves is recommended. Percenta Synthetic-Sealing dehumidifies the skin. The application should be checked at an inconspicuous spot or a sample.

Not to be applied at temperatures below +5°C.

Preparation:

The surface has to be cleaned carefully from dusty, greasy and fatty pollutions. It is recommended to use Percenta Universal Cleaner. To remove the remains of the tensides, it should be rinsed intensively with clear water. Before coating the surfaces must be clean, dry and non-greasy.

Coating:

The coating will be carried out by rubbing or polishing with a cotton-towel, humidified with Percenta Synthetic-Sealing. (The Percenta polishing-towel is perfect.). The material should be spread over the clean surface sparingly and with rotating gestures. (You require approx. 10-25 ml per m²).

IMPORTANT:

The drying of the applied material requires 15 minutes at least. If the humidity is higher, an extension of the cure time is to be expected (up to several hours).

The treated surface will be polished afterwards only.

Proof of effectiveness through drop-test

On the whole surface the water should form drops, not a regular coating.

Drying:

The „Easy-to-Clean“ effect appears approx. 30 minutes after polishing.

If the temporary Easy-to-Clean effect fades, you can proceed in the same way as with the first treatment.