Percenta - Soil sealing for low- to non-sucking subsoils

Percenta SOIL SEALING is a coating material for soil-resisting and abrasive-resistent components of mineral subsoils. Nano particles in the coating effect an evidently increased lifetime of the coating. PERCENTA SOIL SEALING provides protection against clay and ground, against pollution with wet leaves, oil and food, like coffee for example.

Dilution:	none

Quantity to be applied:	approx. 10-20 ml per m²

Curing / Drying:	approx. 8 hours at minimum, preferably 24-48 hours

Handling:	refer to safety data sheet

Storing and durability:	refer to safety data sheet, imprint on bottles or cans

(storing temperature: +5°C  to +25°C, to be protected against direct insolation and frost, to be stored well closed in the original container)

Application:

The carrying of gloves is recommended. Percenta soil-sealing dehumidifies the skin. The application should be checked at an inconspicuous spot or a sample.

Not to be applied at temperatures below +5°C.

Preparation:

The surface has to be cleaned from dust and dirt. For this purpose please use a cleaner usually in trade and rinse again with water.

Coating:

Per square meter approximately 10-20 ml are necessary, which can be sprayed on, rolled up or applied by paint brush.

Drying:

At room temperature the surface of the coating is dry after approx. one hour after the applying, and will be hardened completely after approx. 1-2 days. Coated base plates can be re-entered after approx 1-2 hours.

Cleaning of the coated surface:

In case of pollution, the coated surfaces should be cleaned with water and brush, furthermore a cleaner usually in trade or a high-pressure cleaner can be used additionally, if required.