# Percenta textile-sealing

Areas of application:

Seats, car tops, carpets, textiles, gloves, shoes, leather combs, saddlebags, rainwear, umbrellas, leather, suede, upholstered furniture, sun blinds, tents ...

Percenta textile-sealing is an aqueous impregnation for textiles and papers for hydrophoby (water-repellent) and oleophoby (oil-repellent). The product forms a nearly invisible, think surface coat around the fibre. Due to the hydrophobic effect, the humidity penetration rate of treated textiles or papers as well as the newl pollution, for example with soot or coffee, will be reduced considerably.

Percenta textile-sealing is resistant to dry-cleaning.

Dilution:	none

Quantity to be applied:	approx. 10-100 ml per m² (depending on the types of textiles)

Curing / Drying:	approx. 1 hour at minimum, preferably 24 hours

Handling:	refer to safety data sheet

Storing and durability:	refer to safety data sheet, imprint on bottles or cans

(storing temperature: +5°C  to +25°C, to be protected against direct insolation and frost, to be stored well closed in the original container)

Application:

Shake very intensively before use. It is recommended to use a spraying application (for example hand-sprayer) or immerse or roller application respectively. The application should be checked at an inconspicuous spot or a sample.

Preparation:

Before the application the textiles must be washed and rinsed intensively, to remove all textile additives or  finishing facilities (for example surface-active agents and slip additives).

Coating:

Percenta textile-sealing should be applied in that way, that a thin, regular wet coat on the surface of the textile will be formed. Depending on the thickness of the applying, a flimsy shading of the textiles can appear.

Drying:

Drying should be done at room temperature (at least 1 hour, or until the material feels dry) or through thermal drying up to 160°C in the drying tunnel or in the circulating air drier. Alternatively the material can be dried with the iron only.